1. Copper Cathodes (Grade A)

Standard: ASTM B115 (Grade 1) or LME Grade A (BS EN 1978).

Target Market: Cable, wire, and electronics manufacturing.

Vietnam Note: Buyers almost exclusively demand LME Registered brands. Non-registered brands usually trade at a significant discount.

| Parameter | Limit | Typical Value |
| --- | --- | --- |
| Purity (Cu) | Min 99.9935% | 99.99% - 99.999% |
| Oxygen (O) | ASTM E2575 | Max 0.0005% (5 ppm) |
| Sulfur (S) | ASTM E2575 | Max 0.0015% (15 ppm) |
| Iron (Fe) | ASTM E2575 | Max 0.0010% (10 ppm) |
| Silver (Ag) | ASTM E2575 | Max 0.0025% (25 ppm) |
| Dimensions | - | 914mm x 914mm x 12mm (approx) |

2. Copper Concentrates

Standard: No fixed ASTM; sold on contractual assay.

Target Market: Smelters.

Vietnam Note: Crucial. Vietnam has strict limits on "deleterious elements." If Arsenic is too high, the cargo may be rejected as "hazardous waste."

| Parameter | Standard Method | Typical Specification |
| --- | --- | --- |
| Copper (Cu) | ISO 10258 | Min 25% (Base grade) |
| Gold (Au) | Fire Assay | 1 – 20 g/mt (Payable credit) |
| Silver (Ag) | Fire Assay | 30 – 200 g/mt (Payable credit) |
| Arsenic (As) | ISO 13545 | Max 0.5% (Penalty triggers >0.2%) |
| Fluorine (F) | Ion Selective | Max 300 - 500 ppm |
| Mercury (Hg) | CV-AAS | Max 10 ppm (Very strict) |
| Moisture | ISO 10251 | Max 8 - 10% (Transport limit) |

3. Copper Ore

Standard: Geological assay.

Target Market: Processing plants (less common to trade raw ore internationally due to freight costs, but high-grade ore is traded).

| Parameter | Typical Spec | Notes |
| --- | --- | --- |
| Copper (Cu) | 10% - 15% | Direct shipping ore (DSO) high grade. |
| Size | 0 - 10 mm | Fines or Lumps (contract specific). |
| Moisture | Max 8% | To prevent liquefaction during shipping. |
| Impurities | - | Must comply with Vietnam's environmental "allowable waste" limits if not fully refined. |

4. Aluminum (Ingots) & Bauxite

Context: Vietnam has the world's 2nd largest Bauxite reserves. They generally export Alumina/Bauxite. However, they import refined Aluminum Ingots (P1020) for manufacturing. I have provided the spec for Ingots, as this is the likely import trade.

A. Aluminum Ingots (Primary)

Standard: ASTM B179 or LME P1020A.

| Parameter | Limit |
| --- | --- |
| Aluminum (Al) | Min 99.7% |
| Iron (Fe) | Max 0.20% |
| Silicon (Si) | Max 0.10% |
| Zinc (Zn) | Max 0.03% |
| Form | Ingots, T-Bars, or Sows. |

B. Bauxite (Metallurgical Grade - if trading)

- $Al_2O_3$ (Alumina): Min 45-50%

- $SiO_2$ (Silica): Max 5% (Reactive silica is the penalty element)

- Moisture: Max 10%

5. Lithium (Battery Grade)

A. Lithium Carbonate ($Li_2CO_3$) – Battery Grade

| Parameter | Unit | Standard Limit | Typical Value |
| --- | --- | --- | --- |
| Purity ($Li_2CO_3$) | % | Min 99.50 | 99.60 |
| Sodium (Na) | % | Max 0.025 | 0.015 |
| Calcium (Ca) | % | Max 0.005 | 0.003 |
| Iron (Fe) | % | Max 0.001 | 0.0005 |
| Silicon (Si) | % | Max 0.003 | 0.001 |
| Chloride (Cl-) | % | Max 0.003 | 0.001 |
| Sulfate (SO4) | % | Max 0.010 | 0.005 |
| Moisture ($H_2O$) | % | Max 0.250 | 0.150 |
| Magnetic Impurities | ppb | Max 300 | < 100 |
| Particle Size (D50) | µm | 3.0 – 8.0 | 5.5 |

B. Lithium Hydroxide ($LiOH \cdot H_2O$) – Battery Grade

Preferred for high-nickel cathodes (NCM 811) used in advanced EVs.

| Parameter | Unit | Standard Limit | Typical Value |
| --- | --- | --- | --- |
| Purity (LiOH) | % | Min 56.50 | 57.10 |
| Carbon Dioxide ($CO_2$) | % | Max 0.35 | 0.25 |
| Sodium (Na) | % | Max 0.002 | 0.001 |
| Potassium (K) | % | Max 0.001 | 0.0005 |
| Calcium (Ca) | % | Max 0.005 | 0.003 |
| Iron (Fe) | % | Max 0.0005 | 0.0003 |
| Magnetic Impurities | ppb | Max 100 | < 50 |
| Acid Insolubles | % | Max 0.005 | 0.002 |

6. Zinc & Lead Concentrates

A. Zinc Concentrate

| Parameter | Unit | Rejection Limit (Vietnam/China Ref) | Typical Commercial Spec |
| --- | --- | --- | --- |
| Zinc (Zn) | % | Min 45.0% | 50.0% – 55.0% |
| Silver (Ag) | g/mt | - | 50 – 150 (Payable) |
| Gold (Au) | g/mt | - | 0 – 2 (Payable if >1g) |
| Iron (Fe) | % | Max 12.0% | 5.0% – 9.0% |
| Arsenic (As) | % | Max 0.50% (Strict) | < 0.20% |
| Cadmium (Cd) | % | Max 0.30% | < 0.15% |
| Mercury (Hg) | % | Max 0.01% (100 ppm) | < 0.005% (50 ppm) |
| Silica ($SiO_2$) | % | Max 3.5% | 1.5% – 2.5% |
| Fluorine (F) | ppm | Max 500 | 200 – 300 |
| Moisture | % | Max 9.0% | 7.0% – 8.0% |

B. Lead Concentrate

| Parameter | Unit | Rejection Limit | Typical Commercial Spec |
| --- | --- | --- | --- |
| Lead (Pb) | % | Min 50.0% | 60.0% – 65.0% |
| Silver (Ag) | g/mt | - | 1,000 – 2,500 (High Value) |
| Zinc (Zn) | % | Max 7.0% | 3.0% – 5.0% |
| Arsenic (As) | % | Max 0.50% | < 0.30% |
| Bismuth (Bi) | % | Max 0.20% | < 0.05% |
| Mercury (Hg) | % | Max 0.01% | < 0.005% |
| Moisture | % | Transport Limit | 6.0% – 9.0% |